Title:

Modelling of Multiscale Nonlinear Interaction of Elastic Waves with three dimensional Cracks

Authors: Francesco Ciampa1, Ettore Barbieri2 and Michele Meo1*

1Material Research Centre, Department of Mechanical Engineering, University of Bath, Bath, BA2 7AY, UK

2The School of Engineering and Material Science, Queen Mary, University of London,

Mile End Road, London, E1 4NS, UK

Running title: Multiscale nonlinear wave propagation.

*Corresponding author: m.meo@bath.ac.uk

Abstract

This paper presents a nonlinear elastic material model able to simulate the nonlinear effects generated by the interaction of acoustic/ultrasonic waves with damage precursors and micro-cracks in a variety of materials. Such a constitutive model is implemented in an in-house finite element code and exhibits a multiscale nature where the macroscopic behaviour of damaged structures can be represented through a contribution of a number of mesoscopic elements, which are composed by a statistical collection of microscopic units. By means of the semi-analytical Landau formulation and the Preisach-Mayergoyz space representation, this multiscale model allows the description of the structural response under continuous harmonic excitation of micro-damaged materials showing both anharmonic and dissipative hysteretic effects. In this manner, nonlinear effects observed experimentally such as the generation of both even and odd harmonics can be reproduced. In addition, by using Kelvin eigentensors and eigenelastic constants, the wave propagation problem in both isotropic and orthotropic solids was extended to the three dimensional Cartesian space. The developed model has been verified for a number of different geometrical and material configurations. Particularly, the influence of a small region with classical and non-classical elasticity and the variations of the input amplitudes on the harmonics generation were analysed.

PACS number(s): 43.25.Ba, 43.25.Dc, 43.40.Le

Article

# INTRODUCTION

Ordinary materials such as aluminium, steel, glasses, single crystals and numerous others, exhibit anharmonic effects that can be explained by the classical nonlinear theory of Landau [1], known as Classical Nonlinear Elasticity (CNE). However, in the presence of micro-structural features such as cracks in the medium lattice or fatigue damage, the material nonlinear behaviour may significantly differ from the classical one. In particular, a variety of materials such as rocks, soil, ceramics, sandwich structures, concrete, metal alloys with mesoscopic flaws (i.e. with a characteristic length smaller than the wavelength) can become highly nonlinear and manifest quasi-static and dynamics effects such as hysteresis and discrete memory in the stress-strain relationship [2], [3], [4]. Hence, despite of their very different microstructure, the stress-strain relationship of these materials obeys to a new class of media known as Nonlinear Mesoscopic Elastic (NME).

Nonlinear elastic effects of damaged materials can be usually assessed with nonlinear elastic wave spectroscopy (NEWS) [5], [6], [7], [8] and phase symmetry analysis (PSA) techniques [9], which explicitly interrogate the material nonlinear elastic behaviour and its effect on wave propagation caused by the presence of defects. A number of experimental tests were performed on a wide variety of materials subjected to micro-damages in different environmental conditions. In particular, using either mono- or a bi-harmonic excitation, the material acts as a nonlinear mixer so that when the harmonic waveforms interact together at the damage location, not only their superposition, but also sum and difference frequencies, in addition to higher harmonics, and sub-harmonics of the fundamental frequencies and can be generated [10], [11]. These new frequency components indicate that a flaw is present within the material. Differences between NME and CNE nonlinear dynamic behaviour include quadratic amplitude dependence with the third harmonic of NME materials versus cubic in the classical ones, and a downshift of the fundamental frequency, proportional to the resonance amplitude in the NME media versus quadratic amplitude dependence with the second harmonic predicted by the CNE theory [12], [13].

In the last decade a number of analytical approaches have been developed to significantly simplify the problem, but they may not succeed in reproducing the whole set of observed phenomena. Hence, the application of numerical calculations can be used as an alternative for a more complete theoretical analysis, including the extension of a basic 1D model to higher dimensions [14]. Nevertheless modelling wave propagation and the material response in micro-cracked solids with classical and non-classical material nonlinear behaviour presents significant challenges. Hirose and Achenbach [15] numerically solved the dynamic problem of contacting crack faces due to incident wave motion using the boundary element method (BEM). In the field of wave propagation in conjunction with a spring model, Delsanto and Scalerandi [16] developed the local interaction simulation approach (LISA) to investigate the influence of nonlinear elasticity on the 1D and 2D dynamic wave propagation in materials with hysteresis stress-strain relations at the microscale. However, the LISA model treats every inhomogeneity (grain boundary, micro-crack, etc…) individually by modelling the splitting of a node into two sub-nodes with specific characteristics that define its mechanical stress-strain relation. This is very demanding on the calculation time and not very practical when dealing with large systems or extension to higher dimensions (order of 1012 microscale features per cm3).

To reduce calculation demands, it is advantageous to introduce an intermediate level between the microscopic mechanics and the macroscopic behaviour. This intermediate or mesoscopic level can be regarded as the element level as generally used in finite element (FE) or finite difference (FD) methods. Therefore, based on these considerations, a new model was developed by Guyer et al. [17] based on the Preisach-Mayergoyz (PM) space representation, in analogy with the treatment of magnetic hysteresis. In particular, at the mesoscopic level, each material element can be thought as composed of a statistical ensemble of microscopic features with elementary hysteretic operators [18]. Hence, a multiscale model for nonlinear and hysteretic wave propagation, involving microscopic, mesoscopic and macroscopic levels, appears to be far more efficient and has potential for being used in simulations of higher dimensional geometries and inverse modelling techniques. Van Den Abeele et al. [19], [20] proposed a combination of elastodynamic finite integration technique (EFIT) and PM space for a 1D resonant bar and a 2D isotropic material with localized damage. Zumpano and Meo [21] and Barbieri et al. [22], [23] used the PM space formalism to evaluate the nonlinear response of a damaged medium with a finite element and a meshless element free Galerkin method, respectively.

This paper presents the development of a nonlinear elastic material model, implemented in an explicit in-house FE numerical software, able to simulate the nonlinear interaction of acoustic/ultrasound waves with micro-cracks. Such a constitutive model has a multiscale nature where the macroscopic behaviour of damaged solids is represented through a contribution of a number of mesoscopic elements, which are composed by a statistical collection of microscopic units. In this manner, nonlinear effects observed experimentally such as the generation of both odd and even harmonics associated to material hysteresis and anharmonic effects, respectively, can be simulated. In addition, by means of Kelvin eigentensors and eigenelastic constants, the 1D and 2D nonlinear wave propagation problem in both isotropic and anisotropic structures was extended to the 3D Cartesian space. Hence, this research work can be considered as a general framework for the study of the macroscopic nonlinear response of micro-damaged materials such as metals, composites and alloys that may show both nonlinear classical and non-classical effects. The layout of this paper is as follows: in Section II, the 3D multiscale nonlinear elastic model is theoretically presented. Section III illustrates the numerical results in terms on nonlinear responses for two different structures, a 3D isotropic and orthotropic bar and a 3D orthotropic plate. Finally, conclusions are drawn and summarised.

# 3D MULTISCALE MODEL FOR NONLINEAR WAVE PROPAGATION

Following a multiscale concept, the macroscopic response is here considered depending on a finite number of mesoscopic material elements (order of 1-10 mm) that in turn are composed by a large number of microscopic units (order of 1-100 m) with varying properties defining their stress-strain relation. By means of the semi-analytical Landau formulation and the PM space representation, this multiscale model allows the description of the structural (macroscopic) response under continuous periodic (harmonic) excitation of micro-damaged materials showing both anharmonic effects and dissipative hysteretic losses.

## Material Constitutive Model

At the microscale level, the total scalar strain response, , of each unit can be modelled through a combination of a classic nonlinear component, Cl, that takes into account the anharmonic effects in CNE materials, and a non-classical addition H because of the hysteresis and discrete memory effects [19]

εTOT=εCl+εH.	(1)

Hence, introducing the nonlinear classical stress, C, and the non-classical counterpart, H, the inverse of the total nonlinear elastic modulus, KTOT, of the microscopic unit is (Fig. 1)

1KTOT=1KCl+1KH=∂εCl∂σCl+∂εH∂σH.	(2)

The theoretical model on nonlinear interaction of acoustic/ultrasonic waves with the structural defect can be treated in CNE materials as an expansion of the elastic energy as a power series with respect to the strain, Cl. Thus, according to Landau’s nonlinear classical theory [1], the inverse of the elastic modulus, KCl, in CNE materials becomes

1KCl=∂εCl∂σCl=1K01+βεCl+δεCl2+⋯,	(3)

where K0 is the linear elastic modulus and  and  are classical second order and third order nonlinear coefficients. In order to evaluate the inverse of the elastic modulus contribution in NME media, the PM formulation was used [24]. In this phenomenological state relation, the strain contribution at the microscale level equals either zero or a finite value, , depending on the actual stress value, , and its history, his.

In particular, for positive stress rate ∂σ/∂t>0, the strain contribution is zero for σ<σc (“open” state) and for σ>σc (“closed” state) (Fig. 1). The constant γ=εc−εorepresents the total strain jump when the microscopic unit switches from “open” to “closed”. For negative stress rate ∂σ/∂t<0, the strain contribution equals  for σ>σO (“closed” state) and zero for σ<σO (“open” state). In this case, γrepresents the total strain jump when the microscopic unit switches from “closed” to “open”. Naturally is σc>σO and only the parameters σc and σO can vary from unit to unit. Physical dynamic models attribute this non-classical nonlinear behaviour to the closure and opening of bond system between grains or the friction of crack surfaces [25], [26].

In the up-scaling from microscopic to mesoscopic level, the linear elastic modulus, K0, and the nonlinear coefficients  and  can be assumed as constants within a material mesoscopic element. Hence, Eqs. (2) and (3) still maintain their effectiveness at the mesoscopic level and can be used to predict the nonlinear classical elastic modulus KCε. Moreover, in order to quantify the hysteresis and discrete memory effects at mesoscopic level, the method proposed by Aleshin et al [27] was used. In particular, the mathematical implementation of the PM space model is associated with the stress pairs σc,σO and the mesoscopic element density distribution, μσc,σO, with σc,σO∈σmin,σmax. In other words, in the continuum limit (109-1012 units/cm3) the density, μσc,σO, is used as a measure of the fraction of mechanical units within the material mesoscopic element that are in a “closed” or “open” state at the stress, σ.

Thereby, following the ideas of the PM space formalism, the nonlinear non-classical contribution to strain can be represented through a linear superposition of statistical ensemble of N individual hysteretic units located at position x

εHx=N∈xεN,	(4)

where εN corresponds to the nonlinear strain of each hysteretic unit. By using Eq (2) and replacing the summation over all elements in Eq. (4) with integration over the entire PM space, the non-classical correction of the elastic modulus can be obtained as follows:

∂εH∂σσ,σ=−∞+∞dσO−∞+∞dσcμσc,σO∂εN∂σ,	(5)

in which according to Fig. 2

∂εN∂σ=−γδσ−σc if state=open ∂σ/∂t>0δσ−σO if state=close ∂σ/∂t<00 if state=close ∂σ/∂t>0,	(6)

where γ=Nγ. Assuming a uniform distribution of the elementary hysteretic units within the PM space, we can interpret μσc,σO as the number  of mechanical elements (per unit of volume) with control parameters σc,σO belonging to the interval σO,σO+dσO and σc,σc+dσc

μσc,σO=const=μ.	(7)

Hence, Eq. (5) becomes

∂εH∂σσ,σ=μ−∞+∞dσO−∞+∞dσc∂εN∂σ.	(8)

A graphical illustration of the hysteresis element switching procedure is plotted in Fig. 2(a)-2(f), which contains a series of snapshots of the PM space, corresponding to different points of the stress curve in Fig. 2(g).

By examining the evolution of  over time, the elementary microscopic units are closed for  and the associated strain is zero. Increasing the stress to point A’ [Fig. 2(g)], all the units contained in the area of the PM space (associated to the mesoscopic element) defined by the triangle OAB close [Fig. 2(a)]. The strain variation becomes:

∂εH∂σσ↑,σhis=−γμ−∞σΩdσO	(9)

where Ω=1 if the region containing the microscopic units is open and Ω=0 if it is closed. Eq. (9) represents the contribution of the inverse of the nonlinear hysteretic elastic modulus of the elementary units closing at the actual stress, . The separation between the closed and open area (known as switching line) is determined by the actual value of the stress. In the case illustrated in Fig. 2(a), as the stress rate is positive, the switching line is vertical and the black arrow indicates the direction of switching. Bringing the stress value to σA, all the microscopic units enclosed in the trapezium ABCD close as well [Fig. 2(b)]. Reducing the stress to σB, all the units having a value of the stress higher than σB open [see dashed triangle CEF in Fig. 2(c)]. Since now the stress rate is negative ∂σ/∂t<0, the strain variation corresponds to a simple line integral in the PM-space over a horizontal line segment. Thereby, for negative stress rate, Eq. (8) reduces to

∂εH∂σσ↓,σhis=−γμσ+∞Ωdσc,	(10)

where Ω=1 if the hysteretic units are closed and Ω=0 if the hysteretic units are at open state. Unlike Eq. (9), Eq. (10) represents the contribution of the inverse of the nonlinear hysteretic elastic modulus of the mesoscopic element containing microscopic units that are opening at the actual stress, . Then the stress is further reduced to the point B’ [Fig. 2(d)]. A subsequent increase of stress to σc determines the closing of the hysteretic units enclosed in the triangle GIL [Fig. 2(e)]. As a result, the integration along the switching line defined by −∞<σc<σ reduces to the integration along the switching section defined by the points I and L. Hence, Eq. (9) becomes

∂εH∂σσ↑,σhis=−γμLσΩdσO.	(11)

A following decrease of stress to point D determines the opening of the units closed at the previous stage. In this manner, the level of stress recorded at σD=σB is reinstated and the material memory property is reproduced. The further reduction and increase of the stress in accordance with the stress protocol of Fig. 2(g) determine the closure and opening of the hysteretic units of the individual mesoscopic element [Fig. 2(f)]. The ensembles of switching sections define the material history line, which is used to directly evaluate the hysteretic contribution to the material elastic modulus. Hence, the analytical nonlinear non-classical elastic behaviour defined by Eqs. (9), (10) and (11) can be described through the following equations:

1KHσ,σhis=γAoσ,σhisAtot1σ if ∂σ∂t>0	(12)

and

1KHσ,σhis=γAcσ,σhisAtot1σ if ∂σ∂t<0,	(13)

where γ (constant) is the maximum strain for all the unit cells closing and opening in the PM space, Atot=σmax−σmin2/2 is the total area of the PM space and Acσ,σhis and Aoσ,σhis are the contributions of the hysteretic units in a “closing” and “opening” state, respectively. Since Eqs. (12) and (13) are associated to the sign of the stress rate, the non-classical nonlinear elastic modulus is highly dependent on the stress history his.

## Kelvin Notation for 3D Orthotropic Elastic Media

The model described above to obtain the nonlinear classical and non-classical elastic moduli is a scalar model, so it cannot be directly used to solve 3D problems. To overcome this limitation, Kelvin notation was used to extend the standard Voigt stress-strain formulation in a tensorial equivalent form for a 3D Cartesian space [28]. In particular, the stress and strain second-rank tensors in the 3D space for a homogeneous orthotropic elastic medium are closely connected to each other by the following 6 x 6 stiffness matrix in Voigt notation:

σ11σ22σ33σ23σ13σ12=K11K12K13000K12K22K23000K13K23K33000000K44000000K55000000K66ε11ε22ε33ε23ε13ε12	(14)

or

σ=Kε.	(15)

Introducing Kelvin notation, Eq. (15) can be rewritten in the form

σ=Kε,	(16)

where the shearing components of these new six-dimensional (6D) stress and strain vectors are multiplied by 2:

σ=σ11,σ22,σ33,2σ12,2σ13,2σ23Tε=ε11,ε22,ε33,2ε12,2ε13,2ε23T,	(17)

and K is a new six by six matrix:

K=TKT with T=I002I.	(18)

The symmetric matrix K can be shown to represent the components of a second-rank tensor in a 6D space. We consider now the eigenvalue problem obtained by seeking those strain states for which σ and ε are parallel in the 6D space. Specifically, the eigenvalues of the matrix K are the six numbers  that satisfy the following equation [29]:

K−ΛIε=0.	(19)

Since the 6D linear transformation K[Eq. (18)] is assumed to be symmetric and positive definite, there will be a maximum of six positive eigenelastic constants associated to Eq. (19) known as Kelvin moduli. These eigenvalues will be denoted by Λi, i=1,…,6 and ordered by the inequalities Λ1≥Λ2≥⋯Λ6>0. In addition to the six values of Λ, also six values of ε will be associated to the problem (19), which are denoted by the vector εi in the 6D space. The stresses σi obtained by multiplying εi by the eigenvalues Λi are called the stress eigentensors. A Cartesian basis in the 6D space can be constructed from the normalized strain eigentensors, denoted by N

ε=Nε; ε2=ε⋅ε; N⋅N=1.	(20)

Hence, the stress eigentensors can be written in terms of the normalized strain eigentensors using Eqs. (16), (19) and (20) as

σi=Λiεi.	(21)

With respect to the 6D space, σ, εand K have the following representation:

σ=i=16Λiεi=i=16ΛiεiNi,ε=i=16εi=i=16εiNi,	(22)

and:

K=i=16ΛiNi⊗ Ni,	(23)

where ⊗ indicated the tensor or dyadic product. For orthotropic symmetry, there are nine distinct elastic constants, K11, K12, K13, K22, K23, K33, K44, K55 and K66 and six distinct eigenvalues Λi with i=1,…,6. The last three eigenvalues associated with Eq. (19) are

Λ4=2K44; Λ5=2K55; Λ6=2K66	(24)

and their associated eigenvectors become

ε4=N4=000100Tε5=N5=000010Tε6=N6=000001T.	(25)

The first three eigenvalues of Eq. (19) satisfy the following relation:

K11−ΛK12K13K12K22−ΛK23K13K23K33−Λε1ε2ε3=0.	(26)

By decomposing the determinant of Eq. (26), we obtain an algebraic equation of the third power with respect to Λ

Λ3−Λ2X1+ΛX2+X3=0.	(27)

The solution of the characteristic equation defined above is valid for orthotropic but also isotropic materials, by simply imposing the particular case of K11=K22=K33=+2, K12=K13=K23=, K44+K55+K66=2, with  and  the Lame parameters. The eigenvalues associated with the characteristic equation (27) are

Λ1=X13+X5X6+X6,	(28a)

Λ2=X13−12X6+X5X6+X7,	(28b)

Λ3=X13−12X6+X5X6−X7.	(28c)

The normalized eigenstrains associated to the eigenvalues Λk with k=1,2,3 are

N1=11+Y112+Y122Y11Y121000T,N2=11+Y212+Y222Y21Y221000T,N3=11+Y312+Y322Y31Y321000T,	(29)

where the coefficients X1, X2, X3, X4, X5, X6, X7 and X8 for the evaluation of the eigenvalues [Eq. (28)] and the coefficients Y11, Y12, Y21, Y22, Y31, Y32 for the evaluation of the eigentensors [Eq. (29)] are reported in the Appendix. The normalized eigenvectors defined by Eq. (25) simple represent shearing in the symmetry planes, whilst the eigentensors defined by Eq. (29) represent simple extension or contractions along the various symmetry planes. The projection of the stress-strain state given by Eq. (17) along these eigenvectors define the eigenstress vector σ and the eigenstrain vector ε. Their components are reported in Eq. (A10) of the Appendix.

By using the eigenvalues and eigentensors defined in Eq. (A10), the total elastic modulus due to nonlinear classical and non-classical effects defined in Eq. (2) becomes

1KTOT,i=1Λi1+βεi+δεi2+⋯+1KH,iσi,σhis.	(30)

Once the total elastic modulus KTOT,i (i=1,…,6) is obtained, according to Eqs. (30) and (23) the nine elastic moduli can be modified from Kelvin to Voigt notations follows:

K11TOT=Y1121+Y112+Y122KTOT,1+Y2121+Y212+Y222KTOT,2+Y3121+Y312+Y322KTOT,3	,(31a)

K12TOT=Y11Y121+Y112+Y122KTOT,1+Y21Y221+Y212+Y222KTOT,2+Y31Y321+Y312+Y322KTOT,3	,(31b)

K13TOT=Y111+Y112+Y122KTOT,1+Y211+Y212+Y222KTOT,2+Y311+Y312+Y322KTOT,3	,(31c)

K22TOT=Y1221+Y112+Y122KTOT,1+Y2221+Y212+Y222KTOT,2+Y3221+Y312+Y322KTOT,3	,(31d)

K23TOT=Y121+Y112+Y122KTOT,1+Y221+Y212+Y222KTOT,2+Y321+Y312+Y322KTOT,3	,(31e)

K33TOT=11+Y112+Y122KTOT,1+11+Y212+Y222KTOT,2+11+Y312+Y322KTOT,3	,(31f)

K44TOT=KTOT,42,	(31g)

K55TOT=KTOT,52,	(31h)

K66TOT=KTOT,62.	(31i)

Therefore, the 6 x 6 nonlinear stiffness matrix KTOT of the mesoscopic element obtained using Eq. (31) will be used for the implementation of the explicit FE numerical method at each individual time step. Moreover, based on the model represented above, the symmetry of the material is not affected by the nonlinear effects, as well as the separation of nonlinear behaviour is assumed in the different orientations of the material.

## Nonlinear Finite Element Formulation

In order to solve a multiscale nonlinear structural problem, an explicit finite element (central difference) formulation was used, as it allows computing the nodal forces without recourse to a factorization of the global stiffness matrix in a step-by-step solution. Let us consider a 3D solid domain Ω with boundary  discretized with 3D elements. The weak form of the equilibrium equations for the continuum Ω can be derived from the displacement variational principle as follows [30]:

e=1nelLeTBTσ dΩ−ΦTtdΓ−ΦTb dΩ=0,	(32)

where LeT is the transpose of the Boolean connectivity matrix that gather the nodal displacement, de, of each element e from the global vector, d. over the entire domain, Ω; nel is the total number of elements; Ωe is the element domain;  is the stress second-rank tensor in the 3D Cartesian space, ΦT is the transpose of the shape function matrix; t and b are the surface traction and body force of the element, respectively; and B is the strain nodal displacement matrix defined by

ε=Bde=BLed	(33)

with  the strain second-rank tensor in the 3D Cartesian space. Substituting the nonlinear stiffness matrix of the element [Eq. (31)] into Eq. (32), the internal nodal forces vector, Fint, can be expressed as follows:

Fint=e=1nelLeTfe=e=1nelLeTCeLed,	(34)

where

Ce=BTKTOTB dΩ.	(35)

Moreover, by introducing the inertial body forces through the d’Alembert principle, Eq. (32) becomes

Md=Fext−Fint,	(36)

where the dots superscript denotes a second time derivative operation and the external nodal forces vector and the (lumped) diagonal mass matrix are:

Fext=e=1nelLeTΦTtdΓ+ΦTb dΩ,	(37)

M=e=1nelLeTmeLe,	(38)

with

me=ρΦTΦdΩ.	(30)

The central difference method is based on finite difference expressions for velocity and acceleration at particular instants of time given by:

dn=12Δtdn+1−dn−1,	(420)

dn=1Δt2dn+1−2dn+dn−1.	(41)

Thus n=0, 1, 2, … corresponds to times t=0, t=Δt, t=2Δt, …, where Δt is the time increment. After calculating the response at instant n, time is advanced by Δt, and the response is calculated at instant n+1. Thus, substituting Eq. (41) into (36), the displacement solutions at the step n+1 becomes

dn+1=Δt2M−1Fnext−Fnint+2dn−dn−1.	(42)

In order to start the computations to determine dn+1, the displacement d−1 has to be initially calculated from the values of d0, d0and d0. In particular, d−1 can be determined from a Taylor series expansion about the instant n, for which n=0 and a backward Δt yields:

d−1=d0−Δtd0+Δt2d02.	(43)

The central difference method is conditionally stable, however, if Δt is too large, the computed displacement may become wildly inaccurate and grow without limit. To guarantee numerical stability, the time step used for the simulation satisfy the Courant-Friedrichs-Levy condition [31]:

Δt<Δtcr, Δtcr=2ωmax	(44)

where max is the largest natural frequency of the system. Hence, whilst the time step was selected according to Eq. (44), also the size of the element was chosen in manner so that the propagating waves were spatially resolved. In particular, according to ref. [31] more than 20 nodes per wavelength were used.

The numerical scheme defined by Eqs. (42) and (43) can be used by those elements that present either linear or nonlinear features. Whilst in the former case, the nonlinear elastic moduli are zero, in the nonlinear case the nonlinear stiffness matrix of the element has to be constantly updated at each time step due to the amplitude dependence with the material constants. The multiscale numerical procedure along with the Voigt and Kelvin formulation are illustrated in the flowchart in Fig. 3. In addition, no linear attenuation mechanics was taken into account in this model, even though it can be easily implemented by adding an additional viscous force to Eq. (42) [32].

# NUMERICAL RESULTS

The influence of CNE and NME effects on the multiscale model illustrated above was numerically verified on two different structures, a 3D isotropic and orthotropic bar and a 3D composite plate. All the numerical models were meshed with tetrahedral solid elements using the isoparametric formulation and were implemented in an in-house FE code developed by the authors.

## Results for an Isotropic and Orthotropic 3D Bar

The first numerical model consists of a 3D bar with dimensions of 350 x 17.5 x 17.5 mm3 and is composed of nearly 7000 nodes with more than 30000 elements (with element length of nearly 1.2 mm) (Fig. 4). For the same geometry, both isotropic and orthotropic material properties were considered. In particular, a density of 2700 kg/m3, an elastic modulus of 70 GPa and a Poisson’s ratio of 0.3 were used for the aluminium case, whilst the mechanical properties for the composite bar are reported in Table I, with a lay-up of [0/45/90/-45]s:

Table I: Orthotropic material properties

| E11 (GPa) | E22 (GPa) | E33 (GPa) | G12 (GPa) | G23 (GPa) | G31 (GPa) | 12 | 23 | 31 |  kg/m3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 131 | 9 | 9 | 5.7 | 5.37 | 5.37 | 0.3 | 0.29 | 0/34 | 1545 |

These orthotropic mechanical properties are typically used for aeronautical and civil engineering applications. The bar was modelled in a cantilever position so that it was fixed at one end, whilst the right end was dynamically loaded with a continuous and uniform surface traction force according to the following periodic law:

st=Asin(2πf0t),	(45)

where A is the amplitude of the input source and f0 is the excitation frequency. In both isotropic and orthotropic cases, an amplitude A=1x103 Pa and a fundamental frequency f0=100 kHz were used. The output (displacement) of the numerical model was measured at different locations within a time window of τ=5×10−3s and, according to Eq. (44), the sampling time (time step) was ΔT=1×10−7s for all the numerical models. Figure 5 displays the time histories of the in-plane displacement (for simplicity only the component dx is shown) collected on the top surface of the bar at the coordinate xo=95 mm and yo=8.5 mm for both the isotropic and composite case (the origin xo= 0, yo = 0 is at the left corner of the fixed end).

The micro-cracked zone was assumed as uniformly distributed over a 3D region of dimensions 2 x 12 x 8 mm centred approximately in the middle of the bar (Fig. 4). In this manner, the nonlinear response of the structure to different type of stress waves (shear, longitudinal, etc…) could be simulated. According to Sec. IIC, the nonlinear classical and non-classical behaviour of the material were modelled by imposing the semi-analytical Landau formulation and the PM space representation to those elements within the damaged area. This means that the mechanical behaviour of the elements outside this nonlinear zone was assumed to be purely linear elastic. In order to simulate the harmonics generation in the case of CNE material, only the influence of the even (second) order nonlinear coefficient was considered [Eq. (3)], i.e. =0.6 for the aluminium case and =0.8 for the composite one. Hence, the nonlinear signatures (harmonics generation) could be easily disclosed by analysing the signals in the frequency domain. Figure 6 shows the fast Fourier transformation (FFT) of the in-plane displacement component with a predominant second harmonic contribution in both the aluminium and composite structures.

In order to represent the NME behaviour of the bar, according to Eqs. (12) and (13) the proprieties of the hysteresis were defined by the parameter γ and the stress limits σmax and σmin of the PM space. In our simulations, we assumed β=0, γ=1×10−3 and the stress limits ranging between -5 and 5 MPa for the aluminium case, and γ=1×10−4 and σmax and σmin equal to -6 and 6 MPa for the composite one. Figure 7 illustrates the nonlinear response of the isotropic and orthotropic materials in the frequency domain due to the presence of hysteresis. In both Figs. 6 and 7, the amplitude of second and third harmonic was normalised with that of the fundamental frequency, as in practical situations the coupling between the piezoelectric sensor and the structure as well as the attenuation of the material should be taken into account, which is out of the purpose of this work. In addition, from Fig. 7, it can be clearly seen that due to pure non-classical nonlinear material behaviour, the third harmonic is the most predominant in the measured response. This result is in agreement with the theory and experiments reported by other authors [17], [33], [34], [35]. However, it should be pointed out that additional frequencies within the spectrum in Figs. 6 and 7 are only due to the resonance frequencies of the bar. Furthermore, theoretical and experimental evidences [2], [5] showed that the non-classical and classical material behaviour increase with the amplitude of the excitation signal. In order to investigate this phenomenon, the excitation frequency was kept constant at 100 kHz and the amplitude was ranged between 1x103 and 1x104 Pa. The results in Fig. 8 show a linear pattern of the second and third harmonic dependence with the fundamental amplitude for both isotropic and orthotropic bar. Moreover, the results on the slope of the third harmonic response [Figs. 8(c)-8(d)] are in perfect agreement with those obtained by Vanaverbeke and Van den Abeele [20].

## Results for an Orthotropic 3D Plate

The second geometry used for the nonlinear wave propagation problem was a 3D rectangular plate with dimensions 153 x 106 x 3 mm3 (Fig. 9). The mesh was made of 15000 nodes with 77322 elements in way that the element length was approximately 1 mm. The mechanical properties as well as the stacking sequence were the same as the orthotropic bar reported in Sec. IIIA (see Table I).

However, unlike the previous structure, the dynamical load was provided through an in-plane traction force applied on the plate surface in way to represent the numerical model of two sensors operating in pitch-catch mode. Indeed, a time-dependent uniform pressure distribution, in the form of Eq. (45), was employed to input a continuous harmonic waveform from a circular area centred at xi=110 mm and yi=48 mm on the top surface with radius of 2.5 mm. In this numerical test the values of amplitude and input frequency were A=5x103 Pa and f0=150 kHz. Similarly to the case of 3D bar, the mesoscopic elements with nonlinear features were assumed to be uniformly distributed over a circular area with diameter of 6 mm and thickness of 2 mm located at the middle of the plate. The parameters used for simulating both the nonlinear classical and non-classical material behaviour were =0.9, γ=1×10−4 and σmax and σmin equal to -6 and 6 MPa. Fig. 10 shows the extraction of the nonlinear signature by the FFT of the in-plane displacement dx measured at xi=30 mm and yi=50 mm. As expected, both the second harmonic due to the anharmonic effect and the third harmonic by means of PM space formulation were generated.

It should be noticed that both values of nonlinear coefficients  and γ can be in principle experimentally evaluated through quasi-static or dynamic stress-strain tests [19] or by using a least square optimization algorithms [7]. Particularly, as  strongly depends on the ratio between the amplitude of the second harmonic with the square of fundamental one, it is always less than one [36]. Moreover, the values of the stress limits in the PM space can be assumed equal to the tensile failure strength of the structure. Once this information is available, they can be used as input for nonlinear inverse problems, in which the size of the micro-crack or the fatigue crack growth can be estimated by analysing the variation of the material nonlinear parameters. Future work is on-going to provide experimental confirmation to these theoretical studies.

# CONCLUSIONS

This paper presented a multiscale constitutive material model able to predict the nonlinear effects generated by the interaction of acoustic/ultrasonic waves with damage precursors and micro-cracks. Such a model involved microscopic, mesoscopic and macroscopic structural features and was developed in order to simulate nonlinear classic and hysteretic material response. In particular, by means of nonlinear elastic Landau’s theory and the PM space representation, this multiscale model provided an understanding of phenomena such as the generation of both odd and even harmonics. Moreover, Kelvin formulation was used to extend the wave propagation problem in both isotropic and orthotropic materials from 1- or 2D to the 3D Cartesian space. The above nonlinear multiscale model was implemented in finite element tool. As a result, it was possible to reproduce a number of classical and non-classical nonlinear effects, which were theoretically assumed and experimentally observed in quasi-static and dynamics experiments. In this research work, the numerical cases of a 3D isotropic and orthotropic bar and a 3D orthotropic plate were modelled. Particularly, the influence of the excitation amplitude variations as well as the interactions of stress waves with 3D cracked zone on the harmonics generation was analysed. Therefore, this material model can be a useful tool for the physical interpretation of the nonlinear material effects and for future applications of damage diagnostics.

# APPENDIX:

For the evaluation of the eigenvalues and eigenstrains [Eqs. (28) and (29)] of the stiffness matrix using Kelvin formulation, the following notation has been introduced:

X1=K11+K22+K33	(A1)

X2=K11K22+K11K33+K22K33−K122−K132−K232	(A2)

X3=K11K232+K22K132+K33K122−K11K22K33−2K12K13K23	(A3)

X4=16X1X2	(A4)

X5=X129−X23	(A5)

X6=X4−X1327+X322−X531/2−X4−X1327+X321/3	(A6)

X7=31/2X6−X5X6i	(A7)

X8=K12K132−K232+K13K23K22−K11	(A8)

and

Yk1=1X8[K132K23−K12K33K13+K233−K22K33K23−K23Λk2++K12K13+K22K23+K33K23Λk]Yk2=1X8[K13Λk2−K133−K13K232+K11K33K13+K12K33K23+−K11K13+K12K23+K33K13Λk]	(A9)

The eigenstress and eigenstrain vectors defined in Eq. (22) can be obtained as follows:

ζ1=Y111+Y112+Y122ζ11+Y121+Y112+Y122ζ22+11+Y112+Y122ζ33,	(A10a)

ζ2=Y211+Y212+Y222ζ11+Y221+Y212+Y222ζ22+11+Y212+Y222ζ33,	(A10b)

ζ3=Y311+Y312+Y322ζ11+Y321+Y312+Y322ζ22+11+Y312+Y322ζ33,	(A10c)

ζ4=2ζ23,	(A10d)

ζ5=2ζ13,	(A10e)

ζ6=2ζ12,	(A10f)

with ζ either the stress  or the strain .

References:

- L.-D. Landau, E.-M. Lifshitz, Theory of Elasticity, Chap. III, Pergamon, Oxford, (1986).

- L. Ostrovsky, P.-A. Johnson. “Dynamic nonlinear elasticity in geomaterials”. Riv. Nuovo Cim. 24, 1−46 (2001).

- R.-A. Guyer, P. A. Johnson. “Nonlinear mesoscopic elasticity: evidence for a new class of materials”. Phys Today 52, 30-36 (1999).

- P.-A. Johnson. The Universality of Nonclassical Nonlinearity (with application to Nondestructive Evaluation and Ultrasonics), Chap. 4, Springer New York, 49–69, (2006).

- K. E.-A. Van Den Abeele, P.-A. Johnston, A. Sutin. “Nonlinear Elastic Wave Spectroscopy (NEWS) Techniques to Discern Material Damage, Part I: Nonlinear Wave Modulation Spectroscopy (NWMS)”. Res. Nondestr. Eval. 12 (1), 17-30 (2000).

- M. Meo, G. Zumpano. “Nonlinear elastic wave spectroscopy identification of impact damage on sandwich plate”. Compos Struct 71, 469–474 (2005).

- G. Zumpano, M. Meo. “Damage localization using transient non-linear elastic wave spectroscopy on composite structures”. Int. J. Nonlin. Mech. 43, 217-230, (2008).

- P.-A. Johnson. “The new wave in acoustic testing”. Materials World 7, 544–546 (1999)

- F. Ciampa, M. Meo. “Nonlinear elastic imaging using reciprocal time reversal and third order symmetry analysis”. J. Acoust. Soc. Am. 131 (6), pp. 4316-23 (2012)

- K. E.-A. Van Den Abeele, A. Sutin, J. Carmeliet, P. A. Johnston. “Micro-damage diagnostics using nonlinear elastic wave spectroscopy (NEWS)”. NDT&E International, Vol. 34, 239-248 (2001)

- V.-V. Kazakov, A. Sutin, and P.-A. Johnson. “Sensitive imaging of an elastic nonlinear wave-scattering source in a solid”, Appl. Phys. Lett. 81, 646–648 (2002)

- A. Moussatov, V. Gusev. “Self-induced hysteresis for nonlinear acoustic waves in cracked material”. Phys. Rev. Lett. 90, 124301 (2003)

- J.-A. TenCate, E. Smith, R.-A. Guyer. “Universal slow dynamics in granular solids”. Phys. Rev. Lett. 85, 1020–1023 (2000)

- O. Bou Matar, P.-Y Guerder, Y. Li, B. Vandewoestyne, K. E.-A. Van Den Abeele. “A nodal discontinuous Galerkin finite element method for nonlinear elastic wave propagation”. J. Acoust. Soc. Am. 131 (5), pp. 3650-63 (2012)

- S. Hirose, J.-D. Achenback, “Higher harmonics in the far field due to dynamic crack-face contacting”, J. Acoust. Soc. Am., 93 (1), pp. 142–147 (1993)

- P. Delsanto, M. Scalerandi, “A spring model for the simulation of the propagation of ultrasonic pulses through imperfect contact interfaces”, J. Acoust. Soc. Am., 104, 2584 (1998)

- R.-A. Guyer, K.-R. McCall, G.-N. Boitnott. “Hysteresis, discrete memory and nonlinear wave propagation in rock: a new paradigm”. Phys Rev Lett 74, 3491–94 (1995)

- T. Goursolle, S. Callè, S. Dos Santos, O. Bou Matar. “A two dimensional pseudospectral model for time reversal (TR) and nonlinear elastic wave spectroscopy (NEWS)”. J. Acoust. Soc. Am. 122 (6), 3220–3229 (2007).

- K. E.-A. Van Den Abeele, F. Shubert, V. Aleshin, F. Windels. J. Carmeliet. “Resonant bar simulations in media with localized damage”, Ultrasonics 42 (1-9), 1017-1024 (2004).

- S. Vanaverbeke, K. E.-A. Van Den Abeele. “Two-dimensional modeling of wave propagation in materials with hysteretic nonlinearity”, J. Acoust. Soc. Am., 122, pp. 58–72 (2007).

- G. Zumpano, M. Meo. “A new nonlinear elastic time reversal acoustic method for the identification and localisation of stress corrosion cracking in welded plate-like structures – A simulation study”. Int. J. Solids Struct. 44, 3666–84 (2007).

- E. Barbieri, M. Meo, U. Polimeno. “Nonlinear wave propagation in damaged hysteretic materials using a frequency domain-based PM space formulation”. Int. J. Solids Struct. 46, 165–180 (2009).

- E. Barbieri, M. Meo. “Time reversal DORT method applied to nonlinear elastic wave scattering”. Wave Motion 47 (7), 452–467 (2010).

- I. Mayergoyz. Mathematical Models of Hysteresis and Their Applications, Chap. 2, Elsevier, Amsterdam (2003).

- C. Pecorari. “Adhesion and nonlinear scattering by rough surfaces in contact: Beyond the phenomenology of the Preisach-Mayergoyz framework”, J. Acoust. Soc. Am., 116, pp. 1938–47 (2004).

- V. Aleshin, K. E.-A. Van Den Abeele. “Friction in unconforming grain contacts as a mechanism for tensorial stress-strain hysteresis”, J. Mech. Phys. Solids 55, 765-787 (2007).

- V. Aleshin, V. Gusev, V. Zaitsev. “Propagation of initially bi-harmonic sound waves in a 1D semi-infinite medium with hysteretic non-linearity”, Ultrasonics 42, 1053-1059 (2004)

- K. Helbig and P. N.-J Rasolofosaon. “A theoretical paradigm for describing hysteresis and nonlinear elasticity in arbitrary anisotropic rocks” in Proceedings of the Ninth International  Workshop on Seismic Anisotropy, Society of Exploration Geopysicistry, Tulsa, 383-398, (2000).

- P.-S. Theocaris, D.-P. Sokolis. “Spectral decomposition of the compliance fourth-rank tensor for orthotropic materials” Archive of Applied Mechanics, 70: 289-306, (2000).

- K.-J. Bathe. Finite Element Procedures in Engineering Analysis. Chap. 9, Prentice-Hall Inc., Englewood Cliffs, NJ (1982).

- R.-D. Cook, D.-S. Malkus, M.-E. Plesha. Concepts and applications of finite element analysis, third ed. John Wiley & Sons, New York, pp. 700, (1989).

- J. Donea. Advanced Structural Dynamics, London: Applied Science Publishers, Chap. 4, (1978).

- K. E.-A. Van Den Abeele, K. Van de Velde, J. Carmeliet. “Inferring the degradation of pultruded composites from dynamic nonlinear resonance measurements”, Polym. Compos. 22, 555-567, (2001).

- P.-B. Nagy, L. Adler. “Acoustic Nonlinearity in plastics”, in Review of Progress in Quantitative Nondestructive Evaluation, edited by D. O. Thompson and D. E. Chimenti (Plenum, New York, 1992), Vol. 11, 2025-2032, (1992).

- G. Zumpano, M. Meo. “A new damage detection technique based on wave propagation for rails”. Int. J. Solids Struct. 43 (5), 1023–46 (2006).

- M. Scalerandi, V. Agostini, P.-P Delsanto, K. E.-A. Van Den Abeele, P.-A. Johnson. “Local interaction simulation approach to modelling nonclassical, nonlinear elastic behaviour in solids”. J. Acoust. Soc. Am. 113, 3049 (2003)

Figure captions:

Figure 1 The stress-strain response at the microscale level for materials with both hysteretic and anharmonic effects and PM formulation at microscopic level

Figure 2 Illustration of the switching procedure in the PM space. Increasing the stress from point A’ to point A in the stress curve (g), the microscopic units contained in the trapezoid area ABCD (b) change their state from open to close and contribute to the nonlinear elastic modulus. Then, reducing the stress from point A to B, only the microscopic units that change their state from close to open (the triangle ECF) contribute to the nonlinear elastic modulus (c). This method can be recursively implemented according to the stress history for the single mesoscopic element (d), (e) and (f).

Figure 3 Flowchart of the multiscale numerical model.

Figure 4 Illustration of the geometry of the 3D bar.

Figure 5 Time signals of the in-plane component dx of the displacement for the isotropic (a) and the orthotropic (b) bar measured at the receiver’s location.

Figure 6 FFT of the in-plane displacement from CNE behaviour in the aluminium (a) and composite (b) bar.

Figure 7 FFT of the in-plane displacement from NME behaviour in the aluminium (a) and composite (b) bar.

Figure 8 Second harmonic displacement amplitude versus squared fundamental amplitude for the isotropic (a) and composite (b) bar, and third harmonic displacement amplitude versus fundamental amplitude for the isotropic (c) and composite (d) bar. The load amplitude ranges from 1x103 to 1x104 Pa.

Figure 9 Illustration of the geometry of the 3D plate. Receivers are placed in two different regions on the top surface of the structure. The first is located at x = 52 mm and the y coordinate ranging between 47 and 59 mm, whilst the second is at x = 92 mm and y ranging between 47 and 59 mm.

Figure 10 FFT of the in-plane displacement from CNE behaviour (a) and NME effect (b) on the composite 3D plate.